Advanced Diamond/sp2-bonded Carbon Nanocomposite Materials as Low Threshold Field Electron Emitters

Alexander V. Karabutov, Vitaly I. Konov, Viktor G. Ralchenko, Vadim D. Frolov and Sergey K. Gordeev*)

General Physics Institute of RAS, Vavilova str. 38, Moscow 117942, Russia

*) Central Research Institute of Materials, Paradnaya str. 8, St-Petersburg 191014, Russia

Key words: field electron emission, diamond, carbon nanostructures

# Abstract

Field electron emission from different types of diamond/sp2-bonded carbon nanocomposite materials including diamond/pyrocarbon composites and CVD diamond films is considered as a function of their structure. Uniform emission at low threshold fields of 1-3 V/m was observed for samples with nanocomposite structure, where diamond is combined with a large amount of sp2-bonded carbon phase. On the contrary, the samples with a predominance of diamond or bulk graphite phases emit poorly. A special STM study of the microscopic properties of the emission centers showed that emitted electrons escape from diamond/sp2-bonded carbon interfaces and thin conducting layers with reduced values of the work function. The mechanisms of the low-threshold emission including local field enhancement and decreasing of the tunneling barrier are considered. To describe the emission from the nanocomposite samples it is suggested that one take into account quantum well effects at thin carbon nanolayers and insulator/graphite interfaces.

1. Introduction

During last decade diamond has attracted high research activity in the field of electronic applications and field electron emission(1,2) due to its unique properties such as negative electron affinity (NEA), high thermal conductivity, inertness, and high-yield electron emission. However, high quality diamond as a rule is a good insulator and that makes using diamond in electronics difficult. In particular, high quality CVD diamond films often show poor field electron emission properties.(3-5) One of the ways to improve the electrical conductivity of diamond materials is to incorporate a conductive sp2-bonded carbon phase in the material. Moreover, it has been found that diamond/graphite composed CVD films(5-7) as well as specially designed diamond/carbon nanocomposites(8-10) can demonstrate excellent field electron emission with threshold fields as low as 1-5 V/m. Although incorporated diamond can have a NEA,(11) the role of diamond in the field emission mechanisms for these systems is still not clear enough. Questions include:

- Is the presence of sp2-bonded carbon phase of key importance for the low-threshold electron emission?

- How can the structure of the diamond/sp2-bonded carbon nanocomposites for emission applications be optimized?

- What are the physical mechanisms of emission for these composite systems?

2. Materials and Procedures

We have designed different types of advanced diamond/sp2-bonded carbon nanocomposite materials for low threshold field electron emission. The samples have different grain structures as well as modifications of the sp2-bonded carbon phase. The first type is a novel diamond/pyrocarbon composite (DPC).(8,9) This is a unique model material for studying emission because the composites contain diamond particles covered with thin shells of pyrocarbon. The percentage of the pyrocarbon as well as size of the diamond particles can be controlled over a wide range during the preparation of the samples, so the thickness of the carbon shells can be varied from 0 to some nanometers (Fig. 1). At first, the diamond particles selected by size in a range of 5 nm to 5 m are pressed into disks (typically 20 mm in diameter and 1 mm thick). Then pores between the diamond particles are partially filled by pyrocarbon during a pyrolytic process.(12) The average thickness of the pyrocarbon shells covering the diamond particles is determined by controlling the sp2/sp3 carbon mass ratio during the process in a range from zero (diamond compact) to 0.5. The electrical conductivity of the samples also increases with the ratio. The structure of the DPC was characterized in detail by SEM, TEM, Raman spectroscopy, XPS, XAES, and other techniques.(8,12,13)

Another type of diamond/carbon nanocomposite is represented by CVD diamond films with a controllable amount of nanocrystalline graphite phase.(4,5,14) The films were grown on silicon by d. c. arc-discharge plasma CVD in methane-hydrogen-argon gas mixtures. By changing the CVD growth conditions (gas content, substrate temperature) it is possible to produce films with different diamond quality, grain size, graphite content, resistivity and emission properties.(5)

Three methods were used for the emission study in high vacuum. Macroscopic emission properties (I-V plots, stability and uniformity) were measured with a microprobe device (tungsten 20 m tips positioned at some tens m above the sample surface) as well as a flat 30x30 mm2 phosphor screen placed at 200 m distance above the sample using a glass spacer.(4,9) Threshold emission fields Fth were defined as the value of the field at an emission current of 1 nA. Microscopic properties of the emission centers including surface morphology, field emission intensity, electroresistivity and surface potential (effective work function) were examined with a special scanning tunneling-field emission microscope (STFEM).(15,16)

3. Results and Analysis

For both types of these composites the emission properties strongly depend on the sample structure. The DPC samples demonstrate clear variations of emission properties with sp2-bonded carbon content as well as diamond particles size (Fig. 2). While “pure” nanodiamond compacts emit poorly, the optimized diamond/pyrocarbon ratio allows uniform emission at fields of as low as 1-3 V/m to be observed with an absence of hysteresis in the I-V curves (Fig. 3). Minima (optima) in these dependences of emission thresholds correspond to average pyrocarbon shell thicknesses of 0.4-1 nm. As the structure differs from the optimized one (in both directions), the uniformity of emission sufficiently deteriorates and the threshold field increases (Fig. 2). The same situation is observed when the “optimized” DPC samples are treated in hydrogen plasma. The treatment leads to some etching of the sp2-bonded carbon at the sample surface (as confirmed by micro-Raman spectroscopy and SEM). Again the surface depleted of pyrocarbon exhibits higher emission thresholds and unsatisfactory emission uniformity (Fig. 3, on the right).

A similar trend is observed for CVD diamond films. Samples with an absence or weak presence of sp2-bonded carbon (“pure” diamond films) emit poorly at fields of >30 V/m with hysteresis in I-V plots and activating current jumps for initial cycles (“arc” activation without noticeable surface microdistructions).(4,5) As the films saturate with nanocrystalline graphite (at appropriate growth conditions) the emission improves noticeably: thresholds become as low as 2-5 V/m with better uniformity, and hysteresis/activation disappear. Nevertheless, the best emission properties correspond to a nanocomposite structure of the CVD diamond film, where a coarse-grained diamond phase coexists with a sufficient amount of nanocrystalline graphite.(5) Moreover, samples of highly oriented pyrolytic graphite (HOPG) and bulk glassy carbon (without any traces of diamond phase) show poor emission with hysteresis (Fig. 4). On the other hand, the hydrogen plasma treatment of the well-emitting CVD diamond/graphite films (about 10 samples) again show a deterioration of the emission.(5,16) A corresponding depletion of the surface with graphitic phase during the treatment was confirmed by micro-Raman spectroscopy as well as electroconductivity measurements.

The results of the hydrogen plasma treatment on the well-emitting DPC and CVD diamond/graphite nanocomposites provide evidence against the importance of diamond NEA for the field electron emission from these composites. Indeed, it is well-known that a hydrogen plasma treatment induces NEA of diamond due to hydrogen termination of surface carbon bonds.(11) However, in our numerous experiments with different diamond/carbon systems we did not see marked improvement of the field emission during such treatment. On the contrary, the emission deteriorated which emphasizes the importance of the sp2-bonded carbon nanophases for low-field emission.

To try to understand the nature of the emission sites and the role of diamond and nanocarbon phases in emission, we used high-resolution emission mapping with STFEM. Figure 5 represents maps of topography, field emission intensity, surface potential, and electrical resistivity for a well-emitting DPC sample with 10-100 nm diamond particles. The maps were taken simultaneously at the same 3 x 3 m2 surface area. An emission site (white area) corresponds to a grain agglomerated from a number of smaller diamond particles where there are no high tip-like protrusions. The resistivity at the emission site is relatively high: much higher than for graphite, but smaller than for diamond (insulator). This is rather typical for a semiconductor or thin (two-dimensional, 2D) conductive (graphitic) layers. Since our study showed that only diamond and nanocarbon phases are present in the composites,(8,13) we ascribe the emission region to diamond grains, most probably covered with thin pyrocarbon layers, at least much thinner than the layers on the surrounding surface area. Such an assumption is in good agreement with “as designed” and TEM-shown structure of the composites. Besides, the effective work function (surface potential) is lower in the emitting zones compared to the background (Fig. 5d). The same trends were reported also for the samples with 5 nm diamond particles.(8) Unfortunately, it is difficult to calibrate the resistivity and surface potential scales, so they are given here in arbitrary units.

A detailed STFEM study of the CVD diamond films showed that the emission originates from grain boundaries with lowered work functions and interfaces between the diamond and the graphitic phases possessing interfacial values of electrical conductivity.(5,15-17) The boundaries typically contain a considerable amount of non-diamond phase, and sometimes graphite phase locates both between the diamond grains and on the top of the grains. Similar trends for CVD diamond were also noted by other authors.(18) Thus, it was generally found that the emission of the DPC and the CVD diamond samples is associated just with diamond/sp2-bonded carbon interfaces and thin conducting layers covering the diamond particles or placed between the diamond grains.

4. Discussion

The similarities in the structure of the DPC and CVD diamond films are illustrated in Fig. 6 a,b. The sp2-bonded carbon phase is located between diamond particles (at the grain boundaries). The simplest possible explanation of the emission from carbon and related structures deals with local field amplification by protrusions or columnar grain boundaries with high aspect ratio.(7,19,20) So the field enhancement factor >5000 is necessary to explain the threshold fields of 1 V/m assuming work function value of 5 eV.(9,15) Such large the field enhancement seems unrealistic for the smooth samples studied here. Moreover, if we consider the most favorable case of an atomically sharp protrusion (or a grain boundary) and take into account a logarithmic (not triangular) potential barrier form for the emission from such a tip, we find that the tip must have a height of more than 10 m to provide so high an enhancement factor (see Ref. 15 for details). Such high protrusions were not observed on these samples of DPC and CVD diamond during our SEM and STM studies. Also there are no narrow conducting channels long enough in the insulating diamond matrix in thin (<1 m) CVD film as well as in DPC with 100 nm diamond particles. So the emission can hardly be ascribed to geometric field enhancement only, and a reduction of the tunneling barrier is necessary. On the other hand, the barrier height cannot be as low as 0.02-0.3 eV (compared with a value of 0.03 eV for kBT); otherwise thermionic emission could be observed at room temperature.(20) Thus, a reasonable combination of local field enhancement and lowered work function most probably takes place.

Two basic emission mechanisms, which could take into account barrier reduction in the composites of two carbon nanophases are shown schematically in Fig. 6 c,d. A decrease of the tunneling barrier for escaping electrons can be caused, for example, by covering the diamond with an ultrathin conducting layer, e.g. metals, as found by different authors.(11,21-23) The NEA of “uncoated” diamond also can play an important role. For the mechanism, in which the diamond surface covered by an ultrathin graphitic layer, to be transparent for tunneling (Fig. 6c), electrons are injected from graphite to diamond and then emitted as “diamond electrons” through the barrier, which is lowered due to NEA or band bending (the presence of the NEA for the graphite-coated diamond is assumed to behave similarly to metal coatings(11,21)). The emission area in this case is located on the graphitic surface near the interface and the process is determined, in particular, by the local thickness of the graphitic nanolayer. A second possible mechanism deals with the emission from the NEA diamond surface (exposed to vacuum), where electrons are injected from graphite to diamond,(6,7,21,24) then diffuse to the diamond surface (Fig. 6d). The emission area is located on the diamond surface near the diamond/graphite interface and is limited by the carrier diffusion length in diamond.

To evaluate these mechanisms we assume the most favorable case, in which the position of the Fermi level EF above the diamond valence band maximum Ev is of EF-Ev=1.4 eV as reported for a diamond/graphite Schottky barrier,(25) and the value of NEA is as deep as -2.05 eV.(25) Therefore, the tunneling barrier height is about =2.0 eV. Such a barrier means that for the emission threshold field of 1 V/m an atomically sharp protrusion (or a grain boundary) must be more than 6 m.(15) This seems to be unrealistic for the DPC as well as the CVD diamond films discussed because it was not observed in our numerous studies. Thus, even in the case of the lowest tunneling barrier for diamond due to NEA, it is difficult to find the necessary field enhancement for the well-emitting samples, and therefore the emission mechanisms have a limited application.

Another mechanism of tunneling barrier reduction implies quantum well effects in thin two-dimensional (2D) graphitic nanolayers covering the insulating diamond grains or located between the diamond grains in the DPC (9) and the CVD films.(17,24) The quantum well splitting of the conduction band of a thin semiconducting layer is shown schematically in Fig. 6e. A splitting of the Nth subband of a rectangular 2D well depends on the thickness of the layer, d: EN=EN-EC, as EN=nh2/8md2, where h is Plank’s constant, and m – the effective electron mass. Since the value EN increases as d decreases, the work function of the 2D-layer may be lower than in the bulk case, which could improve emission.

In spite of the bulk graphite and single infinite graphene sheets not being semiconductors, some nanosized forms of sp2-bonded carbon (schwarzites, onion-like clusters, nanotube fragments) can be narrow band gap semiconductors.26,27 As a rule, such carbon nanoclusters have some curvature of their graphite basal planes. In our TEM studies of the DPC we have found that pyrocarbon shells are located around the diamond particles in a similar manner (small curved nanoclusters).(13) In addition, our STFEM study shows that the emitting areas for the DPC and the CVD films have semiconductor-like electrical conductivity (see Fig. 5c and Refs. 9,15-17,24). So the quantum well splitting of the conduction band of the clusters can occur and promote the local reduction of the work function. For example, for a smooth 3D/2D graphite junction appearing on the edge of a graphite coated diamond particle (Fig. 6f) the tunneling barrier for electrons can be reduced to ~1 eV for layers <1 nm thick (using only the first 2D subband for d=0.3 nm (single basal plane), or two subbands for d=0.6 nm (two basal planes)). Such an effective graphite layer thickness is quite typical for DPC and corresponds to good emission properties (see above). Moreover, preliminary calculations made by L. A. Chernozatonskii28 show that the work function on the edge of graphene (single basal plane of graphite) also could be as low as 1 eV.

Assuming the value of the barrier height to be ~1 eV, it is possible to find the necessary value of the field enhancement using a realistic length of protrusion or grain boundary to describe the very low emission thresholds. We emphasize that the quantum well model does not require a NEA of diamond and can be applied to a wide range of carbon materials. Note that the importance of the presence of the fine-structured sp2-bonded carbon in the diamond-based samples for better electron emission was confirmed using soft etching of the graphitic phase in hydrogen plasma. Although the local structure of the sp2-bonded carbon matrix in the composites may be similar to that of pyrolytically produced bulk glassy carbon, the former exhibits superior emission properties (Fig. 4), presumably due to the nanoscale nature of the graphite shell around diamond.

To calculate the dependence of emission current on applied electric field in the 2D model, we first assume that electrons escape from the first subband only (E1). The density Ds(E) of the transverse energy states is -function shaped: Ds(E)=(m/h2) (E-E1). To obtain an analytical solution, the Wentzel-Kramers-Brillioun (WKB) approximation is used as the transmission probability, P(E1,)=exp(-B(-E1)3/2/F), where F is the external electric field,  is the work function of the bulk material, and B=8(2m)1/2/3eh is a constant. Taking into account the dependence EF=EF(F) in the case of a non-degenerate 2D electron gas neglecting field penetration through the 2D gas and integrating using Fermi-Dirac electron statistic (details see Ref. 29), we calculate that electron escape from the first subband J1 is expressed as

J1  J0 exp(-B(-E1)3/2/F),							(1)

where J0=hF/323md2. There is not sufficient difference in the typical values of J0 for this 2D case and the usual 3D Fowler-Nordheim case: they are the same, when =4.8 eV, d=1 nm, and the local electric field F~250 V/m. The main difference originates from the exponential part: the threshold emission field Fth depends on the layer thickness d as

Fth Fth bulk (1-h2/8md2)3/2,							(2)

where Fth bulk=const. At d<1 nm the quantum well effect can influence the emission sufficiently.

Thus, it is unlikely that the low-field electron emission mechanisms for the diamond/sp2-bonded carbon structures can be ascribed solely to specific diamond properties, while the presence of nanostructured sp2-bonded carbon is probably of key importance. Nevertheless, the presence of the diamond phase is desirable to provide the best emission properties achievable due to better thermal conductivity and promoting fine structure formation of sp2-bonded carbon.

5. Conclusion

Diamond/pyrocarbon composites and CVD diamond films with advanced field electron emission properties were considered. The emission at fields as low as 1-3 V/m was observed on the best samples. They typically contain a large amount of sp2-bonded nanostructured carbon phase while samples with a prevalence of the diamond phase emit poorly. Scanning tunneling-field emission microscopy studies showed that the emission is associated with diamond/sp2-bonded carbon interfaces and thin semiconducting layers. Possible mechanisms of low threshold emission including the NEA of diamond were analyzed and it was concluded that the emission for the samples could not be explained by the specific diamond properties. We propose to describe the emission from the samples using quantum well effects on thin carbon nanolayers and insulator/graphite interfaces. The mechanism does not suggest taking into account specific diamond properties, and it may be suitable for a wide variety of sp2-bonded carbon objects.

Figure legends

Fig.1. Schematic structure of the diamond/pyrocarbon composites (DPC).

Fig. 2. Electron emission threshold field vs sp2-bonded carbon content and average diamond particle size for the diamond/pyrocarbon composites. The best emission corresponds to an effective pyrocarbon shell thickness of about 0.4-4 nm.

Fig. 3. Emission I-V curves and site maps for the DPC sample measured with a fluorescent screen before and after surface treatment in hydrogen plasma. A deterioration of the emission after the treatment is observed.

Fig. 4. Field electron emission for “pure” CVD diamond film as well as highly oriented pyrolitic graphite (HOPG) and bulk glassy carbon compared with diamond/carbon nanocomposite materials.

Fig. 5. STFEM mapping of: (a) topography, (b) field emission intensity, (c) electrical resistivity and (d) surface potential for the DPC sample with diamond particle size ranging from 10 to 100 nm showing the low-field emission. The scanning area is 3 x 3 m2.

Fig. 6. Illustrations for a discussion of field electron emission mechanisms. The schematic surface structure of (a) the diamond/pyrocarbon composite and (b) CVD diamond film containing the graphitic phase at grain boundaries. The outer surface may expose uncovered diamond as well as thin or thick graphite layers on diamond particles. Two possible processes of electron tunneling in the composite or diamond film: (c) emission from a diamond surface covered with a thin graphitic layer where electrons are injected from graphite to diamond and then emitted as “diamond electrons” through the barrier, lowered due to NEA or band bending; (d) electrons are injected through graphite/diamond interface (like “back-contact”), and then diffuse to the diamond surface with low or negative electron affinity; (e) the quantum well splitting of the conduction band of a thin 2D graphite layer adjacent to bulk graphite , and (f) the band diagram of low barrier emission for smooth 3D/2D junction of graphite.

## References

1) M. W. Geis, N. N. Efremov, J. D. Woodhouse, M. D. McAleese, M. Marchywka, D. G. Socker and J. F. Hochedez: IEEE Electron Device Lett. 12 (1991) 456.

2) C. Wang, A. Garcia, D. C. Ingram, M. Lake and M. E. Kordesch: Electron. Lett. 27 (1991) 1459.

3) W. Zhu, G. P. Kochalski, S. Jin, L. Seibles, D. C. Jacobson, M. McCormack and A. E. White: Appl. Phys. Lett. 67 (1995) 1157.

4) A. V. Karabutov, V. I. Konov, S. M. Pimenov, V. D. Frolov, E. D. Obraztsova, V. I. Polyakov and N. M. Rossukanyi: J. de Phys. IV C5 (1996) 113.

5) A. V. Karabutov, V. I. Konov, S. M. Pimenov, E. D. Obraztsova, V. D. Frolov, V. G. Pereverzev and A. A. Smolin: J. Wide Bandgap Materials 7 (1999) 68.

6) A. A. Talin, L. S. Pan, K. F. McCarty, T. E. Felter, H. J. Doerrand and R. F. Bunshah: Appl. Phys. Lett. 69 (1996) 3842.

7) F. Lacher, C. Wild, D. Behr and P. Koidl: Diamond Relat. Mater. 6 (1997) 1111.

8) V. Ralchenko, A. Karabutov, I. Vlasov, V. Frolov, V. Konov, S. Gordeev, S. Zukov and A. Dementjev: Diamond Relat. Mater. 8 (1999) 1496.

9) A. V. Karabutov, V. G. Ralchenko and S. K. Gordeev: Technical Digest of the 13th International Vacuum Microelectronics Conference, August 2000 (Guangzhou, China) 128.

10) J. B. Cui, M. Stammler, J. Ristein and L. Ley: J. Appl. Phys. 88 (2000) 3667.

11) P.K. Baumann and R.J. Nemanich: Diamond Relat. Mater. 7 (1998) 612.

12) S. K. Gordeev: p. 1 in Diamond Based Composites  Ed. M. A. Prelas, A. Benedictus, L. T. S. Lin, G. Popovici, P. Gielisse (Kluwer, Dorecht, 1997).

13) A. Vlasov, V. Ralchenko, S. Gordeev, D. Zakharov, I. Vlasov, A. Karabutov and P. Belobrov: Diamond Relat. Mater. 9 (2000) 1104.

14) V. I. Konov, A. A. Smolin, V. G. Ralchenko, S. M. Pimenov, E. D. Obraztsova, E. N. Loubnin, S. M. Metev and G. Sepold: Diamond Relat. Mater. 4 (1995) 1073.

15) A. V. Karabutov, V. D. Frolov, S. M. Pimenov and V. I. Konov: Diamond Relat. Mater. 8 (1999) 763.

16) V. D. Frolov, A. V. Karabutov, V. I. Konov, S. M. Pimenov and A. M. Prokhorov: J. Phys. D: Appl. Phys. 32 (1999) 815.

17) V. D. Frolov, A. V. Karabutov, S. M. Pimenov and V. I. Konov: Diamond Relat. Mater. 9 (2000) 1196.

18) Y. D. Kim, W. Choi, H. Wakimoto, S. Usami, H. Tomokage and T.Ando: Diamond Relat. Mater. 9 (2000) 1096.

19) O. Gröning, O. M. Küttel, P. Gröning and L. Schlapbach: J. Vac. Sci. Technol. B 17 (1999) 1970.

20) V. V. Zhirnov and J. J. Hren: MRS Bulletin 9 (1998) 42.

21) M. W. Geis, J. C. Twichell, J. Macaulay and K. Okano: Appl. Phys. Lett. 67 (1995) 1328.

22) P. W. May, J. C. Stone, M. N. R. Ashford, K. R. Hallman, W. N. Wang and N. A. Fox: Diamond Relat. Mater. 7 (1998) 671.

23) V. I. Polyakov, N. M. Rossukanyi, A. I. Rukovishnikov, S. M. Pimenov, A. V. Karabutov and V. I. Konov: J. Appl. Phys. 84 (1998) 2882.

24) V. D. Frolov, A. V. Karabutov, S. M. Pimenov, E. D. Obraztsova and V. I. Konov: Ultramicroscopy 79 (1999) 209.

25) J. Robertson and M.J. Rutter: Diamond Relat. Mater. 7 (1998) 620.

26) M.-Z. Huang, W. Y. Ching and T. Lenosky: Phys. Rev. B 47, 1593 (1993).

27) J.-C. Charlier and J.-P. Issi: Appl. Phys. A 67, 79 (1998).

28) L. A. Chernozatonskii: private communication, September 2000.

29) V. D. Frolov, A. V. Karabutov, S. M. Pimenov, V. I. Konov and V. P. Ageev: Diamond Relat. Mater. 10 (2001) in press.

Karabutov A. V. et al., Figure 1.

Karabutov A. V. et al., Figure 2.

Karabutov A. V. et al., Figure 3.

Karabutov A. V. et al., Figure 4.

Karabutov A. V. et al., Figure 5.

Karabutov A. V. et al., Figure 6.